## Slide 1: IC Engineering 1
Figures

## Slide 2: Semi Devices

## Slide 3
Isolated Si atoms
decreasing
atom spacing
Si lattice spacing
Electron energy
Electron energy
E
Mostly
empty
Mostly
filled
p
s
n=3
6N p-states total
2N s-states total
(4N electrons total)
N Isolated Si atoms
Electron energy
E
Electron energy
E
4N allowed states
(conduction band)
4N allowed states
(valence band)
Forbidden states
CrystallineSi N-atoms
Fig-semi-dev-band.png
R0 02/19/25
Ref: Fig 2.5 p-28 Pierret
Caption: Conceptual development of the energy band model starting with N isolated Si atoms on the top left, then showing the split bands for Crystalline SI N-atoms and concluding, at bottom right, with the popular version of the energy band model.

## Slide 4
Fig-semi-dev-band.png
R1 03/12/25
Ref: Fig 2.5 p-28 Pierret
Caption: Conceptual development of the energy band model starting with N isolated Si atoms on the top left, then showing the split bands for Crystalline SI N-atoms and concluding, at bottom right, with the popular version of the energy band model.
Electron energy
E
Mostly
empty
Mostly
filled
p
s
n=3
6N p-states total
2N s-states total
(4N electrons total)
N Isolated Si atoms
Electron energy
E
Electron energy
E
4N allowed states
(conduction band)
4N allowed states
(valence band)
Forbidden states
CrystallineSi N-atoms
Isolated Si atoms
decreasing
atom spacing
Si lattice spacing
Electron energy
4N empty states
2N + 2N
filled states

## Slide 5
Few electrons
Wide
(a) Insulator
Thermal excitation moderately easy
(b) Semiconductor
(Room temperature)
Very
narrow
or
(c) Metal
Fig-semi-dev-class.png
R0 02/19/25
Ref: Fig 2.8 p-31 Pierret
Caption: Illustration of the distinction between (a) insulator, (b) semiconductor, and (c ) metal.

## Slide 6
Fig-semi-dev-carrierviz.png
R0 02/19/25
Ref: Fig 2.7 p-30 Pierret
Caption: Visualization of carriers using the bonding model (left) and the energy band model (right) (a) No-carrier situation; (b) visualization of an electron; (c ) visualization of a hole.

## Slide 7
![Electrons move in an electric field. The band diagrams are like figure @fig-semi-dev-class, but with an expanded energy scale showing closely packed levels, each accommodating two electrons. Solid circles show electrons in a level; open circles indicate available levels.](figures/fig-semi-dev-carrier-efield){#fig-semi-dev-carrier-efield}
R0 02/20/25
Ref: Fig 1.2 p-6 Shur

## Slide 8
![Energy band diagrams for a uniform semiconductor sample in (a) zero and (b) non-zero electric field.](figures/fig-semi-dev-band-efield){#fig-semi-dev-band-efield}
R0 02/20/25
Ref: Fig 1.3 p-7 Shur

## Slide 9
![Relationship between band bending and electrostatic variables in a semiconductor: (a) energy band diagram showing band bending; (b) identification of carrier kinetic energies; (c) electron potential energy; (d) electrostatic potential; (e) electric field vs. position from part (a).](figures/fig-semi-dev-band-electrostatic.png){#fig-semi-dev-band-electrostatic}
R0 02/20/25
Ref: Fig 3.10 p-90 Pierret

## Slide 10
![Visualization of (a) donor and (b) acceptor actions via the bonding model. In (a), _Column V_ element P replaces a Si atom; in (b), Column III element B replaces a Si atom.](figures/fig-semi-dev-viz-doping){#fig-semi-dev-viz-doping}
R0 02/22/25
Ref: Fig 2.10 p-36 Pierret

## Slide 11
![(a) Typical temperature dependence of majority-carrier concentration in a phosphorus-doped semiconductor. The plot includes $n_i/N_D$ vs. T (dashed line) for comparison. (b) Qualitative explanation of the concentration-temperature relationship shown in (a).](figures/fig-semi-dev-carrier-vs-t.png){#fig-semi-dev-carrier-vs-t}
R0 02/23/25
Ref: Fig 2.22 p-66 Pierret

## Slide 12
![Visualization of carrier drift: (a) motion of carriers within a biased semiconductor bar; (b) _drifting_ hole on a microscopic or atomic scale; (c) carrier drift on a macroscopic scale.](figures/fig-sem-dev-carrier-drift.png){#fig-sem-dev-carrier-drift}
R0 02/23/25
Ref: Fig 3.1 p-76 Pierret

## Slide 13
![Expanded view of a biased $p$-type semiconductor bar of cross-sectional area $A$.](figures/fig-semi-dev-current-drift.png){#fig-semi-dev-current-drift}
R0 02/23/25
Ref: Fig 3.3 p-77 Pierret

## Slide 14
![Measured carrier drift velocity within ultrapure silicon kept at ambient temperature, analyzing its relationship with the imposed electric field.](figures/fig-semi-dev-drift-vs-efield.png){#fig-semi-dev-drift-vs-efield}
R0 02/23/25
Ref: Fig 3.4p-78 Pierret

## Slide 15
![Visualization of electron and hole diffusion in a macroscopic scale](figures/fig-semi-dev-diffusion.png){#fig-semi-dev-diffusion}
R0 03/12/25
Ref: Fig 3.12 p-95 Pierret

## Slide 16
![Distribution of charge, electric field, and potential for a $p-n$ junction diode (a) when unbiased, and (b) contrast of potential distributions under zero, forward, and reverse bias conditions.](figures/fig-semi-dev-pnjunc.png){#fig-semi-dev-pnjunc}
R0 03/17/25
Ref: Fig 1.4 p-10 Shur

## Slide 17
![Forward-biased junction: (a) distribution of minority carriers on both sides of the transition region, alongside the definitions for distances $x_n$ and $x_p$ measured from the edges of the transition zone; (b) positional variation of the quasi-Fermi levels](figures/fig-semi-dev-pn-current.png){#fig-semi-dev-pn-cuurent}
R0 03/18/25
Ref: Fig 5.15 p-191 Streetman

## Slide 18: Passives

## Slide 19
Fig-passives-res.png R0 01/08/25

## Slide 20
Fig-passives-cap.png R0 01/09/25

## Slide 21
Fig-passives-cap.png R1 01/10/25
+
+
+
+
+
+
+
+
+
+
_
_
_
_
_
_
_
_
_
_

## Slide 22
+
+
+
+
+
+
+
+
+
+
_
_
_
_
_
_
_
_
_
_
_
_
_
_
_
+
+
+
+
+
Fig-passives-cap2.png R0 01/10/25

## Slide 23
+
-
-
+
+
-
+
-
Fig-passives-ind.png R0 01/09/25

## Slide 24
Fig-passives-ind2.png R0 01/09/25

## Slide 25: Linear Ckts

## Slide 26
Fig-circuits-KCL.png R0 01/12/25

## Slide 27
Fig-circuits-KVL.png R0 01/12/25

## Slide 28
Fig-circuits-nodev.png R0 01/12/25

## Slide 29
Fig-circuits-meshi.png R0 01/14/25

## Slide 30
Fig-circuits-sposition.png R0 01/18/25

## Slide 31
A linear circuit with resistors and both dependent and independent sources is connected to a linear or non-linear load
Fig-circuits-linckt.png R0 01/19/25

## Slide 32
Thevenin Equivalent: (a) Disconnect the load and measure the open-circuit voltage. (b) Zero all independent sources to find the equivalent resistance. (c) The Thévenin circuit combines the open-circuit voltage in series with the equivalent resistance.
Fig-circuits-thevenin.png R0 01/19/25

## Slide 33
(a) To determine the short circuit current at the output, we short the load and measure its current. (b) To determine the equivalent resistance, we zero all the independent sources inside the block. (c) The Norton equivalent circuit is formed by putting the short circuit current in parallel with the equivalent resistance, as determined in (a) and (b).
Fig-circuits-norton.png R0 01/19/25

## Slide 34
(a)
(b)
Fig-circuits-maxpower.png R0 01/21/25
(a) Circuit used for max power transfer analysis. (b) Sketch of power delivered to the load as a function of $R_L$

## Slide 35
Fig-circuits-interface.png R0 01/22/25
A general interface circuit and a few examples: (a) Simple pass-through (often omitted), (b) series resistor, (c) parallel resistor, (d) L-pad left, (e) L-pad right